## Slide 1
Conversion of Pine Wood Residue for Enhanced Hydrogen Production via Catalytic Pyrolysis
Presented by MITHAYELANGA MAZITSHANA
(MSc Candidate)
Department of Chemistry
06 – 10 JULY 2026
University of the Western Cape

## Slide 2
ACKNOWLEDGEMENTS
Pyrolysis and catalytic chemistry research group
Dr. A Mabuda
Dr. P Mpungose
Prof. J Görgens

## Slide 3
Introduction
Aim and objectives
Methodology
Results and Discussion
Ongoing work
References
PRESENTATION OUTLINE

## Slide 4
INTRODUCTION
Increasing energy demand and the need to reduce greenhouse gas emissions have accelerated the search for sustainable energy sources.
Hydrogen is a promising clean energy carrier due to its high energy density and zero carbon emissions at the point of use.
However, most hydrogen is still produced from fossil fuel-based processes, resulting in significant carbon emissions.
Biomass offers a renewable and carbon-neutral alternative for sustainable hydrogen production through thermochemical conversion.

## Slide 5
INTRODUCTION
Catalytic pyrolysis has emerged as a promising route for renewable hydrogen production.
Converts the biomass into syngas, bio-oil, and the biochar.

## Slide 6
For the gaseous fraction to be rich in hydrogen, these parameters must be optimized.
Ni(NO3)2, Fe(NO3)2 and Co(NO3)2
Temperature
550, 600, and 650⁰C.
  8-15 %
Lignin and hemicellulose
Pinewood
Particle size: 2-2.5mm
Biomass type
Moisture content
Catalyst
Higher surface-area-to-volume ratio.
Balances dryness to reduce energy loss with enough moisture to preserve quality and stability.
High solubility in water.
Promote gas-forming reactions.
550°C → lignocellulosic components begin extensive secondary cracking.
INTRODUCTION

## Slide 7
AIM AND OBJECTIVES
2. To identify catalysts suitable for enhancing hydrogen production.
AIM:
To optimize a lab-scale pyrolysis system to maximize hydrogen production.
OBJECTIVES:
1. Identifying the optimal conditions for maximum hydrogen yield in a lab-scale pyrolysis system.
3. To determine the effect of pine wood on hydrogen production through catalytic pyrolysis experiments.

## Slide 8
Part I: Biomass preparation
chipping
Pine wood
Chipper
Chips
milling
Retsch mill
sieving
2-2.3mm sieve
METHODOLOGY

## Slide 9
Part III: Impregnation of the catalysts
Ni(NO3)2/Co(NO3)2
DI water
stirring
Magnetic stirrer
Solution
Pine wood
drying
Oven
METHODOLOGY

## Slide 10
Part II: Experimental pyrolysis setup
Pine wood chips
transfer
Sample boat
Pyrolysis setup
Bio-oil
Biochar
Syngas
METHODOLOGY

## Slide 11
Part IV: Breakdown of experimental parameters using 2-factor central composite design (CCD)
METHODOLOGY

## Slide 12
Elemental analysis results of pine wood
CHN - to determine the elemental composition of biomass
RESULTS AND DISCUSSION
Biomass | Weight (mg) | %Nitrogen | %Carbon | %Hydrogen
Pine wood | 10.685 | 0.15 | 42.97 | 6.80
Pine wood duplicate | 10.051 | 0.12 | 43.22 | 8.70
High carbon and hydrogen contents indicate that pine wood is a suitable feedstock for hydrogen production.
The low nitrogen content is advantageous as it minimizes the formation of nitrogen-containing pollutants during pyrolysis.
Duplicate analysis confirmed the reliability of the results.

## Slide 13
Proximate analysis results of pine wood
TGA analysis – to measure how the mass of a biomass sample changes as it is heated.
RESULTS AND DISCUSSION
Below 250⁰C – minimal weight loss due to moisture evaporation.
Between 300 - 380⁰C – Rapid weight loss as hemicellulose and cellulose decompose releasing volatile gases.
Above 400⁰C – Lignin decomposes more slowly promoting secondary cracking and reforming reactions which enhances hydrogen production.

## Slide 14
Basic pyrolysis conditions experimental runs
RESULTS AND DISCUSSION
Increasing the pyrolysis temperature from 600 °C to 650 °C significantly increased H₂ production while reducing CO₂, indicating that higher temperatures favour hydrogen-forming reactions.
CO remained the dominant gas at both temperatures, while CH₄ changed very little; the gas product was mainly composed of H₂, CO, and CO₂.

## Slide 15
Temperature investigation studies at 550, 600, 650ºC using 15wt% catalyst loading
RESULTS AND DISCUSSION
As the temperature increased, CO₂ decreased significantly, while CO remained relatively stable.
This suggests that higher temperatures favour the conversion of CO₂ into hydrogen-rich syngas, improving the overall gas quality for hydrogen production.

## Slide 16
Effect of optimizing the catalyst loading
RESULTS AND DISCUSSION
The addition of the Ni(NO₃)₂ catalyst significantly improved H₂ production compared to the non-catalytic run.
Increasing the catalyst loading from 5 wt% to 10 wt% reduced CO and CH₄ while increasing H₂, but at 15 wt% the hydrogen yield decreased. This suggests that 10 wt% is the optimum catalyst loading.

## Slide 17
Investigating effect of different types of catalysts
RESULTS AND DISCUSSION
Ni(NO₃)₂ catalyst produced the highest hydrogen yield, with the optimum performance at 10 wt%, because nickel is highly active for cracking, reforming, and water-gas shift reactions that promote hydrogen formation while reducing CO.
Co(NO₃)₂ catalyst also enhanced hydrogen production, with the optimum performance at 10 wt%, but it was less effective than Ni(NO₃)₂ because cobalt has lower catalytic activity for hydrogen-producing reactions.

## Slide 18
The elemental analysis confirmed that pine wood is a suitable feedstock for hydrogen production due to its high carbon and hydrogen contents.
TGA analysis showed that moisture was removed below 250 °C, rapid decomposition of hemicellulose and cellulose occurred between 300–380 °C, and lignin decomposed above 400 °C, promoting secondary cracking and reforming reactions that enhance hydrogen production.
Hydrogen production increases when the temperature increases.
Nickel nitrate [Ni(NO₃)₂] demonstrates higher efficiency in hydrogen production due to its strong catalytic ability to break C–H bonds.
The lack of heavier hydrocarbons (C₂–C₄) indicates efficient conversion to lighter gases, favoring a hydrogen-rich gas composition, particularly at higher temperatures.
CONCLUSION

## Slide 19
01
03
02
Analyse the 3rd catalyst results
Calculate the yield of the biochar and bio-oil produced
Calculate the H₂ yield per 20g/biomass
ONGOING WORK

## Slide 20
[1] H. Ishaq, I. Dincer, and C. Crawford, “A review on hydrogen production and utilization: Challenges and opportunities,” Int. J. Hydrogen Energy, vol. 47, no. 62, pp. 26238–26264, 2022.
[2] T. Egeland-Eriksen, A. Hajizadeh, and S. Sartori, “Hydrogen-based systems for integration of renewable energy in power systems: Achievements and perspectives,” Int. J. Hydrogen Energy, vol. 46, no. 63, pp. 31963–31983, 2021.
[3] C. Acar and I. Dincer, “Review and evaluation of hydrogen production options for better environment,” J. Clean. Prod., vol. 218, pp. 835–849, 2019.
REFERENCES

## Slide 21
[4] M. Ni, D. Y. C. Leung, M. K. H. Leung, and K. Sumathy, “An overview of hydrogen production from biomass,” Fuel Process. Technol., vol. 87, no. 5, pp. 461–472, 2006.
[5] M. G. Eloffy et al., “Biomass-to-sustainable biohydrogen: Insights into the production routes, and technical challenges,” Chem. Eng. J. Adv., vol. 12, no. September, p. 100410, 2022.
[6] A. S. N. Huda, S. Mekhilef, and A. Ahsan, “Biomass energy in Bangladesh: Current status and prospects,” Renew. Sustain. Energy Rev., vol. 30, pp. 504–517, 2014.
[7] S. E. Hosseini, M. A. Wahid, and A. Ganjehkaviri, “An overview of renewable hydrogen production from thermochemical process of oil palm solid waste in Malaysia,” Energy Convers. Manag., vol. 94, pp. 415–429, 2015.