## Slide 1
Deep Learning Prediction of the performance of a hybrid CsSn(I1-xBrx)3-based perovskite Lead-free using silicon (Si++) as hole transport layer (HTL)
Presented by: Dr AD KAPIM KENFACK
Electrical characterisation of aluminium-polyaniline Schottky diodes using a machine learning approach.
Masters Student: Hlulani Ndlovu
Supervisor: Prof M Msimanga
Co-Supervisor: Dr AD Kapim

## Slide 2
Introduction & Literature Review
Faculty of science
Department of physics
1
Solar Cells:
Convert sunlight into electrical energy through the photovoltaic effect.
Growing demand for renewable and sustainable energy technologies.
Perovskite solar cells have emerged as promising alternatives due to:
High power conversion efficiency.
Low fabrication cost.
Simple processing techniques

## Slide 3
Introduction & Literature Review
Faculty of science
Department of physics
2
Metal Contacts and Schottky Junctions:
Metal contacts collect charge carriers in solar cells
A metal-semiconductor interface can form a Schottky junction.
The resulting junction properties influence carrier transport and device performance
FTO
PANI
Al

## Slide 4
Introduction & Literature Review
Faculty of science
Department of physics
3
Metal Contacts and Schottky Junctions:
(1) (2
Electrical behaviour is characterized by:
Barrier Height (ΦB)
Ideality Factor (n)
Saturation Current (Is)
Resistance (R)

## Slide 5
Problem Statement
Faculty of science
Department of physics
4
Resistive deposition is a simple and low-cost method for fabricating metallic contacts for Schottky diode devices.
Electrical properties depend on structural parameters such as film thickness and crystallinity
Fabrication and characterization processes can have long iterative turnaround times in device development

## Slide 6
Problem Statement
Faculty of science
Department of physics
5
Thin film fabrication
Functional device
Yes
Good structural properties?
No
Desired electrical properties?
Yes
No
Problem statement
Thin film fabrication
Functional device
Yes
Good structural properties?
No
ML predicted electrical properties
Proposed solution

## Slide 7
Aim & Objectives
Faculty of science
Department of physics
6
Aim: To predict I-V characteristics from structural properties of Al-PANI contacts using a machine learning algorithm.
Objectives:
Fabricate Al- PANI contact layers of different thickness via resistive deposition.
Characterise the Al-PANI contacts (ERDA & I-V Measurements).
Build ML model to predict l-V parameters of Al –PANI contacts based on the thickness of aluminium layer.

## Slide 8
Methodology
Faculty of science
Department of physics
7
PANI Electrodeposition
Aluminum Deposition
ERDA (thickness analysis)
I-V Measurements
I-V Parameters Extraction
Machine Learning Model
FTO Substrate

## Slide 9
Methodology
Faculty of science
Department of physics
8
I-V Parameters Extraction:

## Slide 10
Methodology
Faculty of science
Department of physics
9
Machine Learning Work Flow:
Deposition Al
I-V Experimental data
Parameter Extraction
Data Cleaning + Normalization
Splitting of data (Train/Test)
KNN Regression Model
Prediction of Electrical Parameters
Performance metric (R2, RMSE, Cross-validation)
Neighbour as parameters of the model

## Slide 11
Results and Discussions
Faculty of science
Department of physics
10
Al Depth Profile 160 nm:

## Slide 12
Results and Discussions
Faculty of science
Department of physics
11
Al/PANI/FTO I-V Curves:

## Slide 13
Results and Discussions
Faculty of science
Department of physics
12
Performance Metric Versus K-Neighbours:

## Slide 14
Results and Discussions
Faculty of science
Department of physics
13
Best performance Metric:
Parameters | Values
K-Neighbours | 2
Score Train | 0.9989
Score Test | 0.9971
RMSE Train | 0.01
RMSE Test | 0.021
Cross-Validation | 0.9564

## Slide 15
Results and Discussions
Faculty of science
Department of physics
14
Model Prediction:

## Slide 16
Results and Discussions
Faculty of science
Department of physics
15
Model Prediction:

## Slide 17
Results and Discussions
Faculty of science
Department of physics
16
Model Prediction:

## Slide 18
Results and Discussions
Faculty of science
Department of physics
17
Model Prediction:

## Slide 19
Conclusion
Faculty of science
Department of physics
18
Al/PANI/FTO Schottky contacts were successfully fabricated and characterized, with film thickness determined using ERDA and electrical properties extracted from I–V measurements.
The electrical parameters (ideality factor, barrier height, saturation current, and resistance) were found to be dependent on film thickness, demonstrating the influence of structural properties on device performance.
The K-Nearest Neighbors (KNN) model successfully predicted the electrical characteristics from structural data, demonstrating the potential of machine learning as a tool for faster characterization and optimization of Schottky contacts.

## Slide 20
Faculty of science
13
4. Conclusion and limitations of the model